## Slide 1: Fabrication and Characterization of Composite Materials from Polystyrene, Waste Biomass and Rubber.
Rose Blandith Exantus
Mentor: Dr. Samuel Darko
Summer Undergraduate Research Institute(SURI) 2018

## Slide 2: Background: Uses of Styrofoam Products
Packaging
Construction

## Slide 3: Background: Expanded Polystyrene (Styrofoam)
Some States in the US have banned Styrofoam from waste streams:
San Francisco, California
Washington DC, Washington Seattle
Some cities in New York…

## Slide 4: Background: Challenges and environmental impact
Non- Biodegradable
Expensive transport
Incineration
Air Pollution
Food Contamination
Health concerns

## Slide 5: Current Solutions
Plastic-eating worms may offer solution to our growing polystyrene problem.
Reduce and Reuse.
Mushroom packaging technology.
(Yu Yang, et al.)2015 Environ. Sci. Technol

## Slide 6
Pinecone
Sawdust
Tires Rubber
Additives : 2.5, 5, 7.5, 10, 12.5, 15 grams
Fabrication Experiments
PC + SF composite
SD + SF composite
RB + SF composite

## Slide 7
Fabrication Experiments
Composite Casting
Dried Composite Materials

## Slide 8: Composite Characterization
Density by (dimensions & water displacement)
Absorbability (water submergence)
Tensile strength
Insulation/thermal properties
Nailing /drilling

## Slide 9: Preliminary Results: Density (ρ)
Pinecone
Sawdust

## Slide 10
Preliminary Results: Absorbability
24 HRS water submergence
Counter weight
Sawdust composite
Pinecone composite
Chart: 24 hours
| Styrofoam only | PC 2.5 | SD 2.5 | PC 5 | SD 5 | PC 7.5 | SD 7.5 | PC 10 | SD 10
Before | 33.51 | 32.33 | 34.53 | 36.26 | 36.28 | 37.88 | 39.31 | 47.84 | 39.1
After | 34.81 | 33.86 | 36 | 36.98 | 37.24 | 38.99 | 40.88 | 48.99 | 40.79
1.3g
1.53g
1.11g
1.15g
1.69g
1.47g
0.72g
1.57g
0.96g

## Slide 11
Insulation Property Testing (30oC)
Control
PC composite
SD composite
Aluminum foil boat
Ice cube
Pinecone composite
Sawdust composite
Hot plate
Ice cube
Hot plate

## Slide 12
Preliminary Results: Insulation Properties

## Slide 13: On-going work
Complete fabrication of crab shell composite material.
Complete characterization of all composite materials:
  Density(dimensions, Water displacement),
  Thermal capability,
  Absorbability,
  Tensile strength,
  Insulation.
Crabshell
Rubber

## Slide 14: References
Annenkovaa , E. A., S. A. Tsysar’a, S.A. , & Sapozhnikova, O. A. (2015, March 25). Constructing ultrasonic images of soft spherical scatterers.
Biodegradation and Mineralization of Polystyrene by Plastic-Eating Mealworms: Part 1. Chemical and Physical Characterization and Isotopic Tests retrieved from: https://pubs.acs.org/doi/abs/10.1021/acs.est.5b02661
DePillis, L. (December 18, 2013). You have never actually used a Styrofoam cup, plate or takeout box. Retrieved From: https://www.washingtonpost.com/news/wonk/wp
Frazier, K. How Styrofoam is bad for the environment. Retrieved http://excesslogic.com/recycling-environment/how-styrofoamis-bad-for-the-environment
Kremer, A. (2003, Spring). Cradle to grave: The life cycle of styrofoam. Retrieved from http://flaglerlive.com/wp-content/uploads/Styrofoam.pdf.

## Slide 15: References cont’d
Oliver, C. Styrofoam uses. Retrieved from https://www.hunker.com/12486063/styrofoam-uses
The danger of Polystyrene (Jul 2010) retrieved from: http://businessbarbados.com/trending/green-business/the-dangers-of-polystyrene/
What is styrene? (2014). Styrene Information & Research Center. Retrieved from www.styrene.org
Yu Yang, et al.(2015)Environ. Sci. Techno retrieved from : https://pubs.acs.org/doi/abs/10.1021/acs.est.5b02663

## Slide 16: Acknowledgments
SURI 2018
Dr. Samuel Darko
Dr. Samir Raychoudhury
Dr. Godwin Mbamalu – DOE-NNSA MISPP CMaEs 2014-2018 Grant
Dr. Charlie Pierce
Dr. Rush Oliver
Research partner: Dahana Durand

## Slide 17
Questions?